Quantitative Results for: Base(13)

| Element | Net Counts | Int. Cps/nA | Weight % | Atom % |
| --- | --- | --- | --- | --- |
| C | 711835 | --- | 4.46 | 7.90 |
| O | 4002101 | --- | 48.28 | 64.24 |
| Na | 129916 | --- | 0.44 | 0.41 |
| Mg | 480650 | --- | 1.08 | 0.95 |
| Al | 729086 | --- | 1.26 | 1.00 |
| Si | 5989252 | --- | 9.26 | 7.02 |
| S | 777962 | --- | 1.08 | 0.72 |
| K | 93873 | --- | 0.16 | 0.09 |
| Ca | 15961039 | --- | 31.55 | 16.76 |
| Fe | 496971 | --- | 2.42 | 0.92 |
| Total |  |  | 100.00 | 100.00 |

Data Type:	Counts

Image Resolution:	512 by 340

Image Pixel Size:	1.68 µm

Map Resolution:	512 by 340

Map Pixel Size:	1.68 µm

Acc. Voltage:	20.0 kV

Magnification:	250

Data Type:	Counts

Image Resolution:	512 by 340

Image Pixel Size:	1.68 µm

Map Resolution:	512 by 340

Map Pixel Size:	1.68 µm

Acc. Voltage:	20.0 kV

Magnification:	250

Data Type:	Counts

Image Resolution:	512 by 340

Image Pixel Size:	1.68 µm

Map Resolution:	512 by 340

Map Pixel Size:	1.68 µm

Acc. Voltage:	20.0 kV

Magnification:	250

Data Type:	Counts

Image Resolution:	512 by 340

Image Pixel Size:	1.68 µm

Map Resolution:	512 by 340

Map Pixel Size:	1.68 µm

Acc. Voltage:	20.0 kV

Magnification:	250

Data Type:	Counts

Image Resolution:	512 by 340

Image Pixel Size:	1.68 µm

Map Resolution:	512 by 340

Map Pixel Size:	1.68 µm

Acc. Voltage:	20.0 kV

Magnification:	250

Data Type:	Counts

Image Resolution:	512 by 340

Image Pixel Size:	1.68 µm

Map Resolution:	512 by 340

Map Pixel Size:	1.68 µm

Acc. Voltage:	20.0 kV

Magnification:	250

Data Type:	Counts

Image Resolution:	512 by 340

Image Pixel Size:	1.68 µm

Map Resolution:	512 by 340

Map Pixel Size:	1.68 µm

Acc. Voltage:	20.0 kV

Magnification:	250