Quantitative Results for: Base(13)

| Element | Net Counts | Int. Cps/nA | Weight % | Atom % |
| --- | --- | --- | --- | --- |
| C | 712163 | --- | 4.61 | 8.29 |
| O | 3670019 | --- | 46.33 | 62.53 |
| Na | 117638 | --- | 0.41 | 0.39 |
| Mg | 476249 | --- | 1.10 | 0.98 |
| Al | 729479 | --- | 1.29 | 1.04 |
| Si | 5989932 | --- | 9.49 | 7.30 |
| S | 777965 | --- | 1.11 | 0.75 |
| K | 93873 | --- | 0.16 | 0.09 |
| Ca | 15961039 | --- | 32.28 | 17.39 |
| Cr | 176764 | --- | 0.68 | 0.28 |
| Fe | 486626 | --- | 2.43 | 0.94 |
| Cu | 11661 | --- | 0.10 | 0.03 |
| Total |  |  | 100.00 | 100.00 |

Data Type:	Counts

Image Resolution:	512 by 340

Image Pixel Size:	0.24 µm

Map Resolution:	512 by 340

Map Pixel Size:	0.24 µm

Acc. Voltage:	20.0 kV

Magnification:	1750

Data Type:	Counts

Image Resolution:	512 by 340

Image Pixel Size:	0.24 µm

Map Resolution:	512 by 340

Map Pixel Size:	0.24 µm

Acc. Voltage:	20.0 kV

Magnification:	1750

Data Type:	Counts

Image Resolution:	512 by 340

Image Pixel Size:	0.24 µm

Map Resolution:	512 by 340

Map Pixel Size:	0.24 µm

Acc. Voltage:	20.0 kV

Magnification:	1750

Data Type:	Counts

Image Resolution:	512 by 340

Image Pixel Size:	0.24 µm

Map Resolution:	512 by 340

Map Pixel Size:	0.24 µm

Acc. Voltage:	20.0 kV

Magnification:	1750

Data Type:	Counts

Image Resolution:	512 by 340

Image Pixel Size:	0.24 µm

Map Resolution:	512 by 340

Map Pixel Size:	0.24 µm

Acc. Voltage:	20.0 kV

Magnification:	1750

Data Type:	Counts

Image Resolution:	512 by 340

Image Pixel Size:	0.24 µm

Map Resolution:	512 by 340

Map Pixel Size:	0.24 µm

Acc. Voltage:	20.0 kV

Magnification:	1750

Data Type:	Counts

Image Resolution:	512 by 340

Image Pixel Size:	0.24 µm

Map Resolution:	512 by 340

Map Pixel Size:	0.24 µm

Acc. Voltage:	20.0 kV

Magnification:	1750