Quantitative Results for: Extracted Spectrum

| Element | Net Counts | Int. Cps/nA | Weight % | Atom % |
| --- | --- | --- | --- | --- |
| C | 692070 | --- | 4.51 | 8.00 |
| O | 3930837 | --- | 48.07 | 64.01 |
| Na | 117454 | --- | 0.41 | 0.38 |
| Mg | 534968 | --- | 1.24 | 1.08 |
| Al | 669730 | --- | 1.19 | 0.94 |
| Si | 6001094 | --- | 9.54 | 7.23 |
| S | 759320 | --- | 1.09 | 0.72 |
| K | 79986 | --- | 0.14 | 0.08 |
| Ca | 15228839 | --- | 30.92 | 16.43 |
| Cr | 170877 | --- | 0.66 | 0.27 |
| Fe | 428392 | --- | 2.14 | 0.82 |
| Cu | 11794 | --- | 0.10 | 0.03 |
| Total |  |  | 100.00 | 100.00 |

Data Type:	Counts

Image Resolution:	512 by 340

Image Pixel Size:	0.24 µm

Map Resolution:	512 by 340

Map Pixel Size:	0.24 µm

Acc. Voltage:	20.0 kV

Magnification:	1750

Data Type:	Counts

Image Resolution:	512 by 340

Image Pixel Size:	0.24 µm

Map Resolution:	512 by 340

Map Pixel Size:	0.24 µm

Acc. Voltage:	20.0 kV

Magnification:	1750

Data Type:	Counts

Image Resolution:	512 by 340

Image Pixel Size:	0.24 µm

Map Resolution:	512 by 340

Map Pixel Size:	0.24 µm

Acc. Voltage:	20.0 kV

Magnification:	1750

Data Type:	Counts

Image Resolution:	512 by 340

Image Pixel Size:	0.24 µm

Map Resolution:	512 by 340

Map Pixel Size:	0.24 µm

Acc. Voltage:	20.0 kV

Magnification:	1750

Data Type:	Counts

Image Resolution:	512 by 340

Image Pixel Size:	0.24 µm

Map Resolution:	512 by 340

Map Pixel Size:	0.24 µm

Acc. Voltage:	20.0 kV

Magnification:	1750

Data Type:	Counts

Image Resolution:	512 by 340

Image Pixel Size:	0.24 µm

Map Resolution:	512 by 340

Map Pixel Size:	0.24 µm

Acc. Voltage:	20.0 kV

Magnification:	1750

Data Type:	Counts

Image Resolution:	512 by 340

Image Pixel Size:	0.24 µm

Map Resolution:	512 by 340

Map Pixel Size:	0.24 µm

Acc. Voltage:	20.0 kV

Magnification:	1750