Quantitative Results for: Neat Batch1 500x

| Element | Net Counts | Int. Cps/nA | Weight % | Atom % |
| --- | --- | --- | --- | --- |
| C | 59507 | --- | 3.98 | 7.09 |
| O | 365195 | --- | 48.70 | 65.04 |
| Na | 4516 | --- | 0.17 | 0.15 |
| Mg | 52666 | --- | 1.28 | 1.12 |
| Al | 58013 | --- | 1.08 | 0.86 |
| Si | 536550 | --- | 8.87 | 6.75 |
| S | 75640 | --- | 1.12 | 0.74 |
| K | 0 | --- | 0.00 | 0.00 |
| Ca | 1564863 | --- | 32.75 | 17.46 |
| Fe | 39844 | --- | 2.06 | 0.79 |
| Total |  |  | 100.00 | 100.00 |

Data Type:	Counts

Image Resolution:	512 by 340

Image Pixel Size:	1.68 µm

Map Resolution:	512 by 340

Map Pixel Size:	1.68 µm

Acc. Voltage:	20.0 kV

Magnification:	250

Data Type:	Counts

Image Resolution:	512 by 340

Image Pixel Size:	1.68 µm

Map Resolution:	512 by 340

Map Pixel Size:	1.68 µm

Acc. Voltage:	20.0 kV

Magnification:	250

Data Type:	Counts

Image Resolution:	512 by 340

Image Pixel Size:	1.68 µm

Map Resolution:	512 by 340

Map Pixel Size:	1.68 µm

Acc. Voltage:	20.0 kV

Magnification:	250

Data Type:	Counts

Image Resolution:	512 by 340

Image Pixel Size:	1.68 µm

Map Resolution:	512 by 340

Map Pixel Size:	1.68 µm

Acc. Voltage:	20.0 kV

Magnification:	250

Data Type:	Counts

Image Resolution:	512 by 340

Image Pixel Size:	1.68 µm

Map Resolution:	512 by 340

Map Pixel Size:	1.68 µm

Acc. Voltage:	20.0 kV

Magnification:	250