Quantitative Results for: Base(5)

| Element | Net Counts | Int. Cps/nA | Weight % | Atom % |
| --- | --- | --- | --- | --- |
| C | 125808 | --- | 5.04 | 8.75 |
| O | 669471 | --- | 49.87 | 64.98 |
| Na | 15127 | --- | 0.32 | 0.29 |
| Mg | 74416 | --- | 1.05 | 0.90 |
| Al | 106783 | --- | 1.16 | 0.90 |
| Si | 1006135 | --- | 9.78 | 7.26 |
| S | 108214 | --- | 0.95 | 0.62 |
| K | 17467 | --- | 0.19 | 0.10 |
| Ca | 2393183 | --- | 29.83 | 15.52 |
| Fe | 58796 | --- | 1.80 | 0.67 |
| Total |  |  | 100.00 | 100.00 |

Data Type:	Counts

Image Resolution:	512 by 340

Image Pixel Size:	1.68 µm

Map Resolution:	512 by 340

Map Pixel Size:	1.68 µm

Acc. Voltage:	20.0 kV

Magnification:	250

Data Type:	Counts

Image Resolution:	512 by 340

Image Pixel Size:	1.68 µm

Map Resolution:	512 by 340

Map Pixel Size:	1.68 µm

Acc. Voltage:	20.0 kV

Magnification:	250

Data Type:	Counts

Image Resolution:	512 by 340

Image Pixel Size:	1.68 µm

Map Resolution:	512 by 340

Map Pixel Size:	1.68 µm

Acc. Voltage:	20.0 kV

Magnification:	250

Data Type:	Counts

Image Resolution:	512 by 340

Image Pixel Size:	1.68 µm

Map Resolution:	512 by 340

Map Pixel Size:	1.68 µm

Acc. Voltage:	20.0 kV

Magnification:	250

Data Type:	Counts

Image Resolution:	512 by 340

Image Pixel Size:	1.68 µm

Map Resolution:	512 by 340

Map Pixel Size:	1.68 µm

Acc. Voltage:	20.0 kV

Magnification:	250

Data Type:	Counts

Image Resolution:	512 by 340

Image Pixel Size:	1.68 µm

Map Resolution:	512 by 340

Map Pixel Size:	1.68 µm

Acc. Voltage:	20.0 kV

Magnification:	250

Data Type:	Counts

Image Resolution:	512 by 340

Image Pixel Size:	1.68 µm

Map Resolution:	512 by 340

Map Pixel Size:	1.68 µm

Acc. Voltage:	20.0 kV

Magnification:	250