## Slide 1
Oklahoma State University & University of Pittsburgh
03.23.2020
Experimental Study of the Triaxial Test of Neat Cement and 0.1% Graphene Cement at Elevated Confining Pressure and Temperatures

## Slide 2
Experimental setup for the triaxial test at elevated temperatures
Test setup & procedures
Stress curve
Mohr-coulomb circle
Preliminary conclusions
Future Works
Syringe pumps for confining load
Temperature & strain change recording
Instron for axial load
Hoek cell wrapped by heat tape

## Slide 3
Experimental setup for the triaxial test at elevated temperatures
Sample before loading into membrane (pre-test)
Assembled Hoek cell wrapped by heat tape with temperature recording system (thermocouple)
Sample in membrane with two strain gauges on side surface
Strain gauge #1
Strain gauge #2
Heat tape
Thermocouple
Test setup & procedures
Stress curve
Mohr-coulomb circle
Preliminary conclusions
Future Works

## Slide 4
Experimental procedures for the triaxial test at elevated temperatures (undrained test)
Test setup & procedures
Stress curve
Mohr-coulomb circle
Preliminary conclusions
Future Works
Glue strain gauges to side surface of sample and place the sample into Hoek cell with membrane. Then, assemble the Hoek cell to loading system.
By using heat tape, increase the system temperature to 90 degree Celsius at very low hydrostatic pressure (~100 psi). This step may take 2 to 2.5 hours.
Increase the isotropic stress of the system to the value of targeted confining pressure.
Follow the ASTM-D7012, start test at constant strain rate (0.2 mm/min) until the sample fails (usually the testing time will be around 10-12 mins).

## Slide 5
Experimental procedures for the triaxial test at elevated temperatures (drained test)
Test setup & procedures
Stress curve
Mohr-coulomb circle
Preliminary conclusions
Future Works
Glue strain gauges to side surface of sample and place the sample into Hoek cell with membrane. Then, assemble the Hoek cell to loading system.
By using heat tape, increase the system temperature to 90 degree Celsius at very low hydrostatic pressure (~100 psi). This step may take 2 to 2.5 hours.
Increase the isotropic stress of the system to the value of targeted confining pressure and waiting the dissipation of the excess pore pressure (may take around 2 hours).
Follow the ASTM-D7012, start test at constant strain rate (0.2 mm/min) until the sample fails (usually the testing time will be around 10-12 mins).

## Slide 6
Triaxial tests lists at elevated temperatures
(up to 3.23.2020):
Test setup & procedures
Stress curve
Mohr-coulomb circle
Preliminary conclusions
Future Works
Sample description | Testing temperature (℃) | Confining pressure (psi) | Drainage condition
Neat cement #1 | 90 | 2000 | undrained
Neat cement #2 | 90 | 6000 | undrained
Neat cement #3 | 90 | 6000 | drained
Neat cement #4 | 90 | 7500 | Failed (membrane damaged)
0.1% graphene #1 | 90 | 2000 | undrained
0.1% graphene #2 | 90 | 6000 | undrained
0.1% graphene #3 | 90 | 7500 | drained

## Slide 7
After increasing CP and before increasing DP
Consolidation period in drained test:
example from neat cement CP @ 6000 psi and 90 ℃ (drained test)

## Slide 8
Test setup & procedures
Stress-strain curve
Mohr-coulomb circle
Preliminary conclusions
Future Works

## Slide 9
Test setup & procedures
Stress curve
Mohr-coulomb circle
Preliminary conclusions
Future Works
F = 5 degree, c = 19 Mpa

## Slide 10
Test setup & procedures
Stress curve
Mohr-coulomb circle
Preliminary conclusions
Future Works

## Slide 11
Test setup & procedures
Stress curve
Mohr-coulomb circle
Post-test failure patterns
Future Works
Preliminary conclusions
Post-test (0.1% graphene @ 2000 psi CP & 90C)
Post-test (0.1% graphene @ 6000 psi CP & 90C)
Post-test (neat @ 6000 psi CP & 90C)
Post-test (neat @ 2000 psi CP & 90C)
Post-test: sample failure patterns
Post-test (0.1% graphene @ 7500 psi CP & 90C)

## Slide 12
Triaxial tests lists at elevated temperatures
(up to 3.23.2020):
Test setup & procedures
Stress curve
Mohr-coulomb circle
Preliminary conclusions
Future Works
Sample description | Testing temperature (℃) | Confining pressure (psi) | Drainage condition | Shear stress at failure (psi)
Neat cement #1 | 90 | 2000 | undrained | 7763
Neat cement #2 | 90 | 6000 | undrained | 11243
Neat cement #3 | 90 | 6000 | drained | 12083
Neat cement #4 | 90 | 7500 | Failed (membrane damaged) | N/A
0.1% graphene #1 | 90 | 2000 | undrained | 9907
0.1% graphene #2 | 90 | 6000 | undrained | 13790
0.1% graphene #3 | 90 | 7500 | drained | 14706

## Slide 13
Under undrained conditions, cement with 0.1% graphene has higher shear strength than neat cement. At the same testing conditions, the shear strength of 0.1% graphene cement is around 15%-25% larger than neat cement.
But this conclusion is currently only limited to the conditions that the confining stress is not higher than 6000 psi and test is under undrained conditions.
Under drained conditions, due to the damaged membrane and limited samples, the data size from both cases are too small to compare. More samples are needed.
Test setup & procedures
Stress curve
Mohr-coulomb circle
Preliminary conclusions
Preliminary conclusions:
Factors may influence the results:
Uneven/rough end surface of sample (main factor)
Long heat and consolidation periods cause the creep of sample

## Slide 14
Test setup & procedures
Stress curve
Mohr-coulomb circle
Preliminary conclusions
Future works:
0.05% graphene cement will be tested at the current conditions to investigate the relationship between increment of concentration of graphene and the change of shear strength.
FLEX cement will also be tested at the current conditions to obtain the shear stress at failure and Mohr-coulomb circle
Micro-structure analysis and/or chemical reactions between graphene and cement may need to be done for explaining the shear strength increment and more ductile strain-stress trend of graphene mixed cement.
Discussion points: