## Slide 1: Raman microscope: Graphene and graphene cement
Cody Massion

## Slide 2: Literature
Literature suggested Raman peaks for cement phases:
Hydrated Portland cement generally consists of:
  calcium silicate hydrate or C-S-H((CaO)1.65(SiO2)(H20)1.75) – 1081, 707, 278cm-1
  portlandite or calcium hydroxide (Ca(OH)2) - 350cm-1
  gypsum (CaSO4 · 2H2O) – 172, 1156cm-1
  ettringite or calcium sulfoaluminate (Ca6Al2(SO4)3(OH)12·26H2O) - 991cm-1
And some unhydrated products like:
  tricalcium silicate (3Ca · SiO2) – 809-936cm-1
  dicalcium silicate (2Ca.SiO2)
  tricalcium aluminate (3Ca · Al2O3) – 504, 757cm-1
  tetracalcium alumino ferrite (4CaO · Al2O3 · Fe2O3).

## Slide 3: Results: Graphene
G
D
2D
Graphene consists of 3 main peaks:
D – ranges from 1300-1400cm-1
G – ranges from 1500-1600cm-1
2D - ranges from 2650-2700cm-1
Ratio of D to G peaks can indicate the amount of impurities found within the graphene, while G to 2D ratio is affected by the number of layers of graphene.
Figure 1 – Raman spot spectrum conducted on as received Platinum graphene nanoplatelets.

## Slide 4: Results: Neat vs 0.1%woc Graphene
Neat Class-H
0.1%woc Graphene
Figure 2 – Raman spot spectrum of hydrated and polished A) Neat Class-H cement B) 0.1%woc graphene added.
A
B
CSH
C3S
CSH
C3A
CH
CSH
C3S
CSH
C3A
CH
C3A

## Slide 5
A
B
C
A
B
C
Figure 3 – Raman area spectrum of 0.1%woc graphene added with 3 different areas selected to compare spectrums.

## Slide 6: Results: 0.1%woc Graphene
Figure 4 – Raman spectrum range of approximately 810-900cm-1 of hydrated and polished 0.1%woc graphene in cement to view and identify large grains.
Large grains appear bright in the range of 810-900cm-1 indicating high intensity of materials in that range. Possible unhydrated cement phases such as C3S, having a spectrum of 809-936cm-1.

## Slide 7
Figure 5 – Raman profilometer 3-dimensional rendering of polished cement surface.
Raman scan of a 200µm by 200µm area of polished 0.1%woc graphene with a depth profile. Dark and nearly black areas indicates pore space within the cement sample. Polished surface roughness is show to be approximately 0.25 to 0.28µm within this area.