## Slide 1: Raman Spectrum and peaks
Olivine
Olivine
The Raman spectrum of this mineral reveals high bending modes from 300 to 650cm-1 and stretching modes between 800 and 1000cm-1.

## Slide 3: Olivine in HCl
2434
3427
3427
2434
964
111
111
111
1
2
3
4
5
6
1
2
3
4
5
6
7
8
9
10
3625 – Stretching vibration of the free OH groups - BY I. PERNOLL AND U. MAIER 1974
175- O…O stretching vibration
No trace of Olivine+
964 not sure what it is?
Figure ***: Raman spectrum and optical image of olivine in HCl. From 10 points scans, seen on (b), there is spectrum(a) appear to have the same composition and no olivine peaks are present. The peaks from 3000-365, depict stretching vibrations of free OH group. Oxygen-Oxygen stretching group is at about 111-175 and peak 2444 is carbon materials.

## Slide 4: Olivine in NaCl
Combine image
3688 – Spectrum of NaCl
Background is red
Figure ***: (a) Raman spectrum, (b) mineral map of olivine in DI-water. The spectrum peaks that need to be identified and The background is black, Red is Olivine and blue is made of 1597 is carbon material
862
828
609
862
3688
2043
1597
(a)
(b)

## Slide 5: Olivine in DI-water
Figure ***: (a) Raman spectrum, (b) mineral map of olivine in DI-water. The spectrum peaks that need to be identified and The background is black, Red is Olivine and blue is made of
Combine image
863
820
1587
1589
1347
609
427
297
(a)
(b)
863
820

## Slide 6: Olivine in Ca(OH)2
863.2
820
2435.2
1087.0
Combine image
1087.0 - Peak for calcium hydroxide
2435.2 – carbon material
Figure1: Three major components are identified: (a) olivine (blue), calcium hydroxide (red), and ***** *(green). The mineral map in (b) shows the distribution of these minerals. Black is the background and blue is olivine, red Ca(OH)2 and green (not sure)
(a)
975.2
(b)