Data was collected after mixing olivine in these different solvents and placing them in an environment chamber with a temperature of 90 0C and relative humidity of 95%

| Olivine in Solutions | pH before olivine addition | pH after Olivine Addition | Taken on 7/11/2020 | Temperature degrees Celcius | Litmus years 7/11/2020 |
| --- | --- | --- | --- | --- | --- |
| Deionized water | 7.58 | 8.59 | 7.75 | 21.9 | 6-7 |
| Sodium Chloride | 9.3 | 7.88 | 7.74 | 22.0 | 7-8 |
| Hydrochloric acid | 1 | 1.92 | 1.75 | 21.9 | 8-9 |
| Calcium Hydroxide | 12.6 | 8.77 | 8.64 |  | 3-4 |
| Oil |  | 7.62 | 5-6 |  | 5-6 |